## Slide 1: Nanoshells under pressure
Pressure gauges with a golden layer
21 July 2012

## Slide 2: Overview
Nanoshells
DAC
Mie & Hybridization theory
Nanoshells (NS) under pressure
Coated Nanoshells (CNS)
Experiments & outview

## Slide 3: Nanoshells: Gifts in a golden wrapper
Dielectric core & metallic shell
Tunable
Au
SiO2
Halas N., Optics & Photonics News, p. 26 (August 2002)

## Slide 4: Nanoshells: Gifts in a golden wrapper
Applications
  Biosensing
  Cancer ablation
  Targeted medication
  Plasmonics
  …

## Slide 5: Diamond Anvil Cell (DAC)
Small pressure on large surface
DAC uses diamonds:
Table
Culet
Notes: Omdat Diamanten hard en onsamendrukbaar zijn. En omdat diamanten doorzichtig zijn, waardoor optische metingen mogelijk zijn.

## Slide 6: Diamond Anvil Cell (DAC)
Create high pressures in between to diamonds
In between the diamonds there is a pressure medium:
  Helium
  Hydrogen
  Neon
  …

## Slide 7: Rubies as pressure sensor
Use the spectrum of rubies to measure the pressure
The R1 and R2 lines will shift under pressure
Needs to be calibrated
APS: http://www.aps.anl.gov/News/APS_News/Content/APS_NEWS_20080311B.php

## Slide 8: Rubies as pressure sensor
Unfortunatly the calibration is not perfect
Interference with diamond resonances
Silvera et. al. Phys. stat. sol. (b) 1, 460-467 (2007)
Notes: Men kalibreert de robijnen via metalen (waarbij men via de roosterparameter zeer nauwkeurig de druk kan bepalen). Echter, zoals uit de figuur blijkt is de kalibratie afhankelijk van het gekozen metaal, wat eigenlijk wil zeggen dat er toch een onnauwkeurigheid zit op de drukmeting

## Slide 9: Nanoshells as pressure gauge
Use the optical response of nanoshells in stead of rubies
Why?
  NS are smaller
  Tunable
  …
Notes: Extra’s: voor opwarming, als extra biosensor, we kunnen ze mixen, …

## Slide 10: Mie-theory
We use Mie-theory to calculate the spectrum of nanoshells:
Rc = 60 nm
Rs = 75 nm

## Slide 11: Hybridization model
Prodan, et. al., Science, 302, 419 (2003)
Nanoshells = cavity + sphere
Solve the Lagrangian of the electron sea which is depicted as an incompresible fluid.

## Slide 12: Mie vs. Hybridization
Mie solves exactly for given dielectric function, but needs further numerical manipulation.
Hybridization is not exact, but gives analytical solutions:

## Slide 13: Nanoshells under pressure
Compression of NS
    Radii change: Rc(P) and Rs(P)
    Electron density changes ne(P)
Vinet equation: J. Geophys. Res. 92, 9319 (1987)
Notes: Vinet equation

## Slide 14: Nanoshells under pressure
Relative cross section:

## Slide 15: Looking good!
We calculate the peak shift:

## Slide 16: Pressure media
SiO2
He
Ne
H2
The nanoshell is not in vacuum, but inside a pressure medium.

## Slide 17: Not so good
The shift changes direction
And seems to stop for He and Ne

## Slide 18: The coated nanoshell (CNS)
Add an extra layer:
  Will shield the influence of the medium
  But leaves the compressiblity
But how thick?
Au
SiO2

## Slide 19: The coated nanoshell
A thick layer is needed!

## Slide 20: Theoretical predictions
Average resolution for CNS: 0,90 nm / GPa
Rubies: 0,36 nm/ GPa
Advantages:
  Nanoshells can be tuned to right frequency band
  Are smaller and need less density
Disadvantage:
  Callibration is still needed

## Slide 21: Experiments
Page left blank intentionally

## Slide 22: Outview
Experimental verification
Finetuning of theory
Heating
Use as biosensor
Sensing of metallic hydrogen

## Slide 23: Nanoshells under pressure
Questions?
21 July 2012
Published: N. Van den Broeck et al. JAP 110, 114318 (2011)

## Slide 24: Extra: waarom geen vol SiO2 bolletje?
R1 = 60 nm
R2 = 75 nm
R3 = 200 nm
R = 200 nm

## Slide 25: Extra: waarom geen Au kern en dikke SiO2 schil?
R1 = 60 nm
R2 = 75 nm
R3 = 200 nm
R1 = 75 nm
R2 = 200 nm

## Slide 26: Extra: waarom geen Au kern en dikke SiO2 schil?